Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/05/15

| Principal investigator |  | Affiliation | King Mongkut’s University of Technology Thonburi |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Lecturer Dr. |  |  |
|  |  | Name | Somporn Peansukmanee |  |  |
| Collaborated researcher of ILM |  | Affiliation | Toyama Center for Advanced Aluminum Materials Research and International Collaboration |  |  |
|  |  | Job title | Prof. Dr. |  |  |
|  |  | Name | Toshiya Shibayanagi |  |  |
| Title of the joint research |  | Weldability and Metallurgical Characteristics of Sn-Treated Recycled Aluminum Alloys |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | SEM : Scanning Electron Microscope STEM: Scanning Transmission Electron Microscope |  |  |  |
| Total amount of grant | Travel expense（ 280,000 JPY） |  |  | Consumable Fee ( 20,000 JPY） |  |
| Research Results 【The major results】 The project has successfully demonstrated the technical feasibility of joining Sn-treated recycled aluminum alloys through pulsed laser and arc welding trials. We are currently refining a specialized casting process that utilizes tin (Sn) to facilitate silicon (Si) separation within the metal matrix. Furthermore, the core research concept—focusing on the "Extended Life Cycle" of aluminum through repair—was presented at the International Symposium "Aluminum Resource Circulation" at the University of Toyama in November 2025, where it received significant interest and positive academic feedback. 【Future Prospects】 The upcoming phase will prioritize the optimization of casting parameters to eliminate current inconsistencies in Si distribution, ensuring a uniform material for more comprehensive testing. We plan to conduct high-resolution metallurgical characterization at ILM using Scanning Electron Microscopy (SEM) and Scanning Transmission Electron Microscopy (STEM) to analyze the weld metal and heat-affected zones. This analysis will be critical in establishing the precise correlation between Sn-content, microstructural evolution, and the overall mechanical performance of the joints. 【Concrete results】 ●Invited lecture The project has successfully established the technical feasibility of joining Sn-treated recycled aluminum through pulsed laser and arc welding trials. We have identified the initial welding parameters and protocols required for these specific alloy compositions. |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |