Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/04/20

| Principal investigator |  | Affiliation | Hanoi University of Science and Technology |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Associate Professor |  |  |
|  |  | Name | Pham Mai Khanh |  |  |
| Collaborated researcher of ILM |  | Affiliation | University of Toyama |  |  |
|  |  | Job title | Associate Professor |  |  |
|  |  | Name | Seungwon Lee |  |  |
| Title of the joint research |  | Effect of Cu on precipitation behavior of Al-Mg-Si extrusion alloys |  |  |  |
| Joint research Program ※check the box |  | X □ Program for Joint Usage / Research Centers (JURC) □ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | X □ Focused themes □ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | HRTEM（EM-002B, Topcon, University of Toyama）、STEM（Talos 200X G2, Thermo Fisher Scientific, ARC in University of Toyama） |  |  |  |
| Total amount of grant | Travel expense （ 240,000 JPY） |  |  | Consumable Fee（ 60,000 JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 Al-Mg-Si alloys are widely used as extrusion materials for building materials, among other applications, due to their high specific strength, excellent formability, and good corrosion resistance due to anodizing. In extrusion materials, strengthening effects due to processing and grain refinement are expected, and even better mechanical properties can be achieved by applying appropriate aging treatment. In this research, we were to improve the mechanical properties of 6000 series aluminum alloys by controlling their structure and analyzing the formation behavior of precipitates and their effects in detail. Our found out that the additive elements, aging temperature, aging time, and processing conditions were strongly affected to the morphology and distribution of precipitates using a transmission electron microscopy (TEM). 【Future Prospects】 In recent years, there has been an increased focus on reducing CO₂ emissions due to global environmental concerns. As a result, more stringent regulations are anticipated in Europe by 2030. In response to these strengthened environmental regulations, the automobile industry is promoting fuel efficiency and electrification. As part of this, weight reduction of vehicle bodies has become an important issue. Aluminum alloys offer a high specific strength, making them a popular lightweight material for replacing steel in various applications. Notably, the 6000 series (Al-Mg-Si system) aluminum alloys have proven particularly effective due to their ability to undergo heat treatment for enhanced strength, making them well-suited for use in structural applications within the transportation sector. Our primary objective is to investigate the effect of added elements on the morphology and distribution of precipitates and to clarify the correlation with mechanical properties. The results of this research will contribute to improving the mechanical properties of 6000 series aluminum alloys through microstructural control and provide fundamental knowledge to expand the range of applications as lightweight structural materials. 【Concrete results】 Co-authored Papers: 1. Effect of pre-deformation on mechanical properties and microstructure of Al-Cu-Mg-Si alloy Vu Ngoc Haia, Seungwon Leea, Taiki Tsuchiyaa, Tetsuya Katsumib, Kazuhiko Kitab, Pham Mai Khanhc, Randi Holmestadd, Calin D. Marioarae and Kenji Matsudaa 2. A comparative investigation of microstructure and mechanical properties in a deformed and aged Al-Mg-Si alloy with high Cu content Vu Ngoc Haia, Abrar Ahmedb, Seungwon Leea, Taiki Tsuchiyaa, Yaofei Zoua, Tetsuya Katsumic, Kazuhiko Kitac, Pham Mai Khanhd, Randi Holmestade, Calin D. Marioaraf, Kenji Matsudaa 3. A comprehensive TEM study on the structure and interfacial characteristics of S’ and S phases in aluminum alloys Vu Ngoc Haia, Abrar Ahmedb,Tetsuya Katsumic, Seungwon Leea, Kazuhiko Kitac, Taiki Tsuchiyaa, Kenji Matsudaa 4. The influence of natural aging on microstructure and hardening behavior during final aging in Al-Mg-Si alloys Tran Sy Quana, Abrar Ahmedb, Pham Mai Khanhc, Vu Ngoc Haia, Susumu Ikenoa, Seungwon Leea, Kenji Matsudaa |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |