Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/07/16

| Principal investigator |  | Affiliation | Norwegian University of Science and Technology, Dept of Physics |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Professor |  |  |
|  |  | Name | Randi Holmestad |  |  |
| Collaborated researcher of ILM |  | Affiliation | University of Toyama, |  |  |
|  |  | Job title | Professor |  |  |
|  |  | Name | Kenji Matsuda |  |  |
| Title of the joint research |  | Age hardening in Al-Zn-Mg alloys with different Zn and Mg additions at constant Zn/Mg ratio. |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) ☑ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | ☑ Focused themes ☑ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | TEM instrument Talos in University of Toyama |  |  |  |
| Total amount of grant | Travel expense（ 240,000 JPY） |  |  | Consumable Fee（ 60,000 JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 PhD student Inga Dahlen Konow visited University of Toyama 10.-20. March 2026 to use the Talos TEM instrument, working together with Prof. Kenji Matsuda, Seungwon Lee, Calin D. Marioara and ….. The grant was used for travel from Norway to Japan and accommodation in the guest house in Toyama university for Inga. We studied precipitates in a 6xxx alloy using the EDS capabilities of the Talos instrument. The goal is to get atomic resolution chemical mapping of the precipitates. 【Future prospects】 The results will be compared with EDS and EELS results in the new instrument at NTNU in Trondheim. The plan is that Inga will make a publication with this results as a part of her PhD thesis. 【Concrete results】 ●Publication – Planned in 2026/2027 ●Conference presentation ●International conference presentation– INALCO, Trondheim June 2026, IMC, Liverpool Sept. 2026 ●Invited lecture - ●Award - ●Acquired external funds etc. |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |