Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/5/12

| Principal investigator |  | Affiliation | Dalian University of Technology |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Assistant professor |  |  |
|  |  | Name | Zhirou Zhang |  |  |
| Collaborated researcher of ILM |  | Affiliation | MRL |  |  |
|  |  | Job title | Professor |  |  |
|  |  | Name | Yoshihito Kawamura |  |  |
| Title of the joint research |  | Study of mechanisms of improved heat resistance of Mg-RE alloys containing LPSO structures caused by kinking bands |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes □ Transportation □ Biomaterials □ Bridge/building materials Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | SEM/EBSD, TEM, in-situ high-temperature mechanical testing, in-situ synchrotron radiation |  |  |  |
| Total amount of grant | Travel expense（200 000JPY） |  |  | Consumable Fee（ JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 Long-period stacking ordered (LPSO) phases strongly influence microstructure and properties in rare-earth Mg alloys, but their role in dynamic recrystallization (DRX) remains unclear. By tailoring the interactions between precipitated LPSO phases and dislocations, this approach not only elucidates the underlying DRX mechanism but also facilitates the development of high-strength magnesium alloys. During tension, confined pyramidal <c+a> slip enhances strength. Zn addition stabilizes grain-boundary eutectics, leading to peak strength in the 1.5Zn alloy (UTS: 476 MPa, YS: 395 MPa) but reduced ductility due to crack propagation. In-situ synchrotron diffraction and tomography reveal distinct deformation and damage mechanisms. These results clarify LPSO–DRX interactions and guide the design of high-performance Mg alloys. 【Future Prospects】 This research aims to clarify the atomic-scale mechanism by which Mn segregation at kink band (KB) interfaces catalyzes precipitation strengthening in Mg-Gd-Y-Zn alloys. We will determine: 1) the precise solute configuration (Mn, Gd) and interfacial energy change at KBs, 2) how this modified interface provides low-energy nucleation sites for β', γ", and CALs phases, and 3) the role of Mn in the spatial and temporal sequence of precipitation during aging to synergistically enhance strength and ductility. 【Concrete results】 ●Publication ●Conference presentation ●International conference presentation ●Invited lecture ●Award ●Acquired external funds etc. |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |