Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/05/14

| Principal investigator |  | Affiliation | Hunan University, China |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Assistant Researcher |  |  |
|  |  | Name | Zhikang Ji |  |  |
| Collaborated researcher of ILM |  | Affiliation | MRC, Kumamoto University |  |  |
|  |  | Job title | Professor |  |  |
|  |  | Name | Michiaki Yamasaki |  |  |
| Title of the joint research |  | Evolution Mechanism of Crack Tip Damage in Heterogeneous Structure Magnesium Alloys |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) ☑ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes ☑ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | SEM, EBSD, Cross Section Polisher (CP), Mechanical testing machine |  |  |  |
| Total amount of grant | Travel expense（300,000JPY） |  |  | Consumable Fee（ JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 Compact tension (CT) specimens of the Mg-Gd alloy were mechanically machined, followed by surface grinding, mechanical polishing, and ion polishing to obtain a surface suitable for SEM and EBSD characterization. A sharp fatigue pre-crack was subsequently introduced using a fatigue testing machine. In-situ tensile tests were then conducted inside the SEM, during which the force–displacement curves were continuously recorded. At selected crack-extension increments, loading was interrupted, and SEM images were acquired to characterize the crack initiation sites and the evolution of the crack propagation morphology. EBSD characterization was performed both in the initial state and after crack extension to obtain information on grain orientation, grain boundaries, and local deformation in the crack-tip region. These experiments established an in-situ and quasi-in-situ characterization procedure for correlating the mechanical response, crack-path evolution, and microstructural characteristics of the Mg–Gd alloy. 【Future Prospects】 In future work, the applied stress-intensity factor, K, and the loading increments will be further calibrated and systematically adjusted to investigate crack-tip deformation and crack propagation under controlled fracture-mechanics conditions. SEM-based digital image correlation will be employed to quantitatively characterize the surface strain distribution and strain localization during crack initiation and propagation. By combining SEM-DIC with in-situ EBSD, the effects of grain size, crystallographic orientation, grain-boundary characteristics, slip-system activation, and slip-transfer compatibility on crack initiation, crack deflection, and fracture toughness will be clarified. In addition, TEM observations will be conducted to characterize the dislocation configurations, dislocation accumulation, and activated slip systems near the crack tip, thereby revealing the microscopic deformation and fracture mechanisms of the Mg–Gd alloy. 【Concrete results】 ●Publication ●Conference presentation ●International conference presentation ●Invited lecture ●Award ●Acquired external funds etc. |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |