Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/05/08

| Principal investigator |  | Affiliation | School of Mechanical Engineering, Pusan National University, Republic of Korea |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Professor |  |  |
|  |  | Name | Taekyung Lee (イ テギョン) |  |  |
| Collaborated researcher of ILM |  | Affiliation | Magnesium Research Center, Kumamoto University, Japan |  |  |
|  |  | Job title | Assistant Professor |  |  |
|  |  | Name | Shin-ichi Inoue |  |  |
| Title of the joint research |  | Preparation and analysis of nonflammable Mg-Al-Ca extruded bars for subsequent electropulsing treatment |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) ■ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes ■ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | Vacuum arc melt furnace, extrusion facility, TEM, and other apparatus for the sample preparation |  |  |  |
| Total amount of grant | Travel expense （300,000 JPY） |  |  | Consumable Fee（ JPY） |  |
| Research Results ※Please describe following three items briefly. 【The Major Results】 EPT enabled rapid temperature control of the Mg-Al-Ca-Mn alloy through Joule heating, reaching approximately 355°C, 380°C, and 407°C under J48 (i.e., current density of 48 A·mm−2), J50, and J52 conditions, respectively. With increasing EPT temperature, the area fraction of C36/C14 compounds decreased from 24.5% (as-cast) to 12.3% (J52), accompanied by an increase in Al concentration and a decrease in Ca concentration within the compounds, suggesting solute redistribution favorable for C15 precipitation. Notably, EPT for only 5 min under J52 induced C15 (Al₂Ca) precipitation comparable to or exceeding that achieved by conventional furnace heat treatment at 400°C for 1 h, demonstrating that EPT is a time-efficient alternative for controlling microstructural evolution in Mg-Al-Ca-Mn alloys. 【Future Prospects】 This collaborative research aims to investigate whether electropulsing treatment (EPT) can serve as a rapid, high-efficiency alternative to conventional furnace heat treatment (FHT) for improving the thermal conductivity of extruded non-flammable Mg-Al-Ca-Mn alloys through controlled C15 precipitate evolution. Unlike as-cast alloys, extruded materials exhibit refined grain structures and redistributed phase distributions, which may significantly influence precipitation behavior and thermal conductivity during subsequent heat treatment. In this study, non-flammable Mg alloys will be fabricated by casting followed by extrusion, and EPT and FHT at approximately 400°C will be applied to the extruded specimens. Thermal conductivity along with microstructural characterization will be measured to evaluate grain structure, phase distribution, and precipitate evolution. 【Concrete results】 - Conference presentation: "Effect of Electropulsing Treatment Parameters on Temperature Profile and Microstructural Evolution of Non-flammable Mg-Al-Ca Alloys" - International research paper to be submitted |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |