Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/MM/DD

| Principal investigator |  | Affiliation | Japan Synchrotron Radiation Research Institute (JASRI) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Research Scientist |  |  |
|  |  | Name | Loku Singgappulige Rosantha Kumara |  |  |
| Collaborated researcher of ILM |  | Affiliation | Advanced Magnesium International Research Center, Kumamoto University |  |  |
|  |  | Job title | Professor |  |  |
|  |  | Name | Yoshihito Kawamura |  |  |
| Title of the joint research |  | In-situ Synchrotron XRD Investigation of Phase Evolution, Texture Changes, and Mechanical Behavior in Mg-Al-Ca Alloys for High-Performance Applications |  |  |  |
| Joint research Program ※check the box |  | ■ Program for Joint Usage / Research Centers (JURC) □ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | ■ Focused themes ■ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | The synthesis equipment for Mg-Al-Ca alloy and film evaluation equipment were supported by the Advanced Magnesium International Research Center at Kumamoto University. |  |  |  |
| Total amount of grant | Travel expense（ 250,000 JPY） |  |  | Consumable Fee（ 50,000 JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 The high-temperature in-situ synchrotron XRD studies examined protective oxide films controlling nonflammability and oxidation resistance in magnesium alloys. In Mg–Al–Ca–Mn, 2θ–sin²Ω measurements showed CaO initially formed at 773 K under tensile stress, then evolved into a CaO/MgO bilayer above 823 K. After melting, inner MgO supported the film while outer CaO developed strong compressive stress, preserving protection. In Mg–Zn–Y and Be-containing Mg–Zn–Y alloys, Y₂O₃ films changed from weak tensile to compressive stress with temperature. Be/BeO segregation at Y₂O₃ grain boundaries blocked oxygen diffusion, increased compressive stress, and improved oxidation resistance. 【Future Prospects】 Future research should focus on designing stable multilayer oxide films that generate beneficial compressive stress during high-temperature exposure and melting. In-situ synchrotron XRD can be extended to wider Mg alloy systems to clarify stress evolution, diffusion paths, and oxide-film failure mechanisms. Optimizing Ca, Y, Be or safer alternative microalloying elements may improve nonflammability while reducing environmental and health concerns. Combining in-situ XRD with TEM, thermodynamic modeling, and oxidation kinetics will support predictive alloy design. These studies can guide development of lightweight, ignition-resistant Mg alloys for automotive, aerospace, and electronics applications requiring reliable oxidation protection at elevated temperatures and improved safety margins. 【Concrete results】 ●Publication 1. S. Inoue, L. S. R. Kumara, Y. Kawamura, Effect of CaO/MgO bilayer film formation on nonflammability and oxidation resistance of Mg–Al–Ca alloys determined by high-temperature in situ residual stress measurement, Corrosion Science, 257, 113311 (2025). 2. S. Inoue, C. Wei Sung, P. Wei Chu, L. S. R. Kumara, Y. Kawamura, Effects of beryllium segregation along grain boundaries of Y2O3 film in Mg–Zn–Y alloy on nonflammability and oxidation resistance, Materials Today Communications 47, 113098 (2025). |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |