Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/05/12

| Principal investigator |  | Affiliation | National Taiwan University |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Assistant Professor |  |  |
|  |  | Name | Shao-Pu Tsai |  |  |
| Collaborated researcher of ILM |  | Affiliation | Kumamoto University |  |  |
|  |  | Job title | Director of Magnesium Research Center / Professor |  |  |
|  |  | Name | Yoshihito Kawamura |  |  |
| Title of the joint research |  | In-situ heating TEM observation on microstructural evolution in Mg alloys |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) ▇ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes □ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening ▇ Independent research theme |
| Name of joint usage apparatus |  | Microscopy facilities |  |  |  |
| Total amount of grant | Travel expense（ 240,000 JPY） |  |  | Consumable Fee（ 60,000 JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 During the joint research period, in-situ heating TEM experiments were successfully conducted on selected Mg alloys using the microscopy facilities at ILM, enabling real-time observation of microstructural evolution over a controlled temperature range. The formation and growth of nanoscale precipitates were directly captured, and their distribution, crystal structure, and orientation relationships with the Mg matrix were clarified at multiple stages by combining aberration-corrected high-resolution TEM with scanning diffraction and EDX/EDS analysis. Temperature-dependent precipitation kinetics were revealed, showing distinct nucleation and growth behaviors at different heating conditions and highlighting differences between grain-interior and grain-boundary precipitation. In addition, the decomposition of metastable solid solutions and successive phase transformations of precipitates were tracked in situ, providing quantitative insight into the evolution of phases during thermal exposure. The role of alloying elements such as Ca, Al, and Zn on grain boundary chemistry and precipitation behavior was qualitatively assessed, indicating their influence on grain boundary cohesion and potential impact on room-temperature ductility. These results establish an experimental framework for in-situ heating TEM studies of Mg alloys and deliver a high-quality dataset that will support further quantitative analysis and publication-oriented work. 【Future Prospects】 Building on the obtained in-situ TEM datasets, future work will focus on quantitative analysis of precipitate nucleation and growth kinetics, including the extraction of characteristic time constants and activation parameters for different thermal conditions. These results will be compared with ex-situ heat-treated specimens and complemented by additional techniques such as EELS, EBSD, and possibly atom probe tomography, with the aim of linking local chemistry and microstructure to macroscopic mechanical properties. The outcomes are expected to lead to one or more journal publications on the microstructural evolution of Mg alloys under thermal loading and to contribute to guidelines for designing heat-treatment schedules. |  |  |  |  |  |