Institute of Light Metals (ILM) Joint Usage/Research Grant Report in FY 2025

2026/04/21

| Principal investigator |  | Affiliation | School of Mechanical Engineering and Mechanics, Xiangtan University |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Job title | Lecturer |  |  |
|  |  | Name | Chang Zhou |  |  |
| Collaborated researcher of ILM |  | Affiliation | International Research Center for Advanced Magnesium, Kumamoto University |  |  |
|  |  | Job title | Assistant Professor |  |  |
|  |  | Name | Shaojie Gu |  |  |
| Title of the joint research |  | Study on uncoupling the electron wind force from Joule heating in electroplasticity |  |  |  |
| Joint research Program ※check the box |  | □ Program for Joint Usage / Research Centers (JURC) ☑ Program for International JURC □ Program for providing samples and materials □ Program for using ILM facilities for sample analysis and characterization |  |  | □ Focused themes ☑ Transportation □ Biomaterials □ Bridge/building materials □ Kink strengthening □ Independent research theme |
| Name of joint usage apparatus |  | FIB FEI Versa 3D, FE-TEM JEM2100F, etc. |  |  |  |
| Total amount of grant | Travel expense（ 250,000 JPY） |  |  | Consumable Fee（ 50,000 JPY） |  |
| Research Results ※Please describe following three items briefly. 【The major results】 - A single helical dislocation is observed to only expand along the radial direction when only subjected to the thermal activation. - At the same temperature, a single helical dislocation gradually evolves into an unfolded morphology and eventually assumes a line-like shape when pulses are applied along its axial direction. Compared with thermal activation results, this phenomenon verifies the existence of electron wind force. - Upon reversing the current direction, the opening direction of the helical dislocation inverses accordingly. This result further corroborates the electron wind force. 【Future Prospects】 In this study, the electron wind force in electroplasticity is successfully decoupled, demonstrating its dominant role in the microstructural regulation of materials. Subsequently, establishing a macro–micro coupled electroplastic constitutive model that accounts for electron wind force will be the core focus. 【Concrete results】 ●Publications - C. Zhou, Z.R. Liu, D. Zhu, S. Hui, L. Zhan, Electric pulse-enhanced dislocation loop reactions to accelerate creep during electrically-assisted compression of an Al-Cu-Li alloy, Materials Science and Engineering: A, 949, 149444 (2026). - J. Chen, C. Zhou*, D. Zhu, L. Zhan, Dislocation loop density-mediated asymmetry of tension-compression creep for an Al-Cu-Li alloy, Journal of Materials Science & Technology, 254, 61-70 (2026). |  |  |  |  |  |
| Notes ・Please use the form and submit to the URL provided in the email by Friday, May 15, 2026. ・The joint research report will be published in the ILM joint research report (annual report) and will be available on our website. Therefore, please prepare the contents for public release accordingly. ・Please add pages, if needed. |  |  |  |  |  |